## Slide 1: Study of Electrochemical Processes for Separation of the Actinides and Lanthanides in Molten Fluoride Media
R. Tulackova (Zvejskova),
K. Chuchvalcova Bimova, P. Soucek, F. Lisy
Nuclear Research Institute Rez plc
Czech Republic

## Slide 2: Motivation of the work (1)
Application of advanced nuclear reactor types for electricity and heat production in the future
Molten Salt Reactor (MSR)
    Th-U breeder (electricty + heat production)
    TRU burner (electricty + heat + transmutation of TRU elements and LLFP) - MSTR
Czech national P&T programme for spent nuclear fuel treatment is focused on development of the Molten Salt Transmutation Reactor (MSTR) fuel cycle system with „on-line“ reprocessing  need of pyrochemical partitioning processes

## Slide 3: Motivation of the work (2)
Pyrochemical partitioning techniques studied in CR:
  Fluoride Volatility Method (FVM)
  Electrochemical separation in molten fluorides
Liquid Fuel Processing Pyrochemical partitioning processes (Electroseparation)
Molten Salt Transmutation Reactor
Uranium
Residual Uranium
Fluoride Volatility Process
Molten Salt / Liquid Metal Extraction and/or Electroseparation
Waste disposal
F2
Spent Fuel
Molten Fluoride Carrier Salt
FP
Pu,MA
Pu,MA,FP
Pu,MA
Pu,MA,FP
residual U,
FP
FP

## Slide 4: Principle of electroseparation method
E – potential of electrode
E0 – red-ox potential of respect ion
R, W, C – reference, working and counter electrode
Used experimental technique:
Linear Sweep Potential Cyclic Voltammetry
Typical scan rate: 50 mV·s-1, working electrode area: ca 2 cm2

## Slide 5: Selection of carrier fluoride melt
Required properties of the melt:
low melting point
high solubility of separated compounds
high electrochemical stability
satisfactory corrosion behaviour
appropriate physical properties (electrical conductivity, viscosity, etc.)
good radiating resistance
Selected melts:
FLINAK – eutectic mixture of LiF-NaF-KF (46.5 - 11.5 - 42.0 mol. %), m.p. 454°C
LiF-CaF2 – eutectic mixture (79.5 - 20.5 mol. %), m.p. 766°C
Raw materials treatment: Desiccation in vacuum drying oven at 60 – 90 – 150 – 250°C

## Slide 6: Experimental set-up
Scan generator MVS 98
KPCI 3102 Keithley
(2 D/A’s)
Potentiostat HP 96 - 20
R
C
Nickel electrolyser providing inert atmosphere in the electrochemical cell
W

## Slide 7: Reference electrode for electrochemical measurement in molten fluorides
Boron nitride main body
Capillary (Ø 0.1 mm)
Carrier melt + NiF2
Nickel wire
Nickel nut
Holders

## Slide 8: Carrier melts
Comparison of voltammograms of pure melts FLINAK  and in LiF – CaF2 



## Slide 9: UF4 in FLINAK and in LiF-CaF2
Comparison of UF4 (1.0 mol. %) voltammograms in FLINAK  and LiF – CaF2 



## Slide 10: Main results of electrochemical measurements
 | FLINAK E [V] vs. Ni/Ni2+ in FLINAK | LiF – CaF2 E [V] vs. Ni/Ni2+ in LiF-CaF2
Cathodic limit | -2.05 V | -2.30 V
Uranium reduction | Two-step reaction –1.20 and –1.75 V | Two-step reaction –1.40 and –1.85 V
Thorium reduction | Two-step reaction –0.70 and –2.00 V | not measured
Neodymium reduction | Two-step reaction –1.00 and < –2.05 V | One-step reaction –2.00 V
Gadolinium reduction | Two-step reaction –1.01 and < –2.05 V | One-step reaction –2.10 V
Europium reduction | Two-step reaction –0.75 and < –1.95 V | One-step reaction < –2.30 V

## Slide 11: Evaluation (1)
The results show the following thermodynamically feasible separation possibilities:
 | Separable | Non-separable
In FLINAK | U / Nd U / Gd U / Th | Th / Nd, Gd, Eu U / Eu Lanthanides among each other
In LiF-CaF2 | U / Gd U / Eu (?) | U / Nd Lanthanides among each other
ACTINIDES ARE LESS ELECTROCHEMICALLY STABLE THAN LANTHANIDES IN BOTH CARRIER MELTS
 Majority of An will be removed prior than Ln (except e.g. Th/Eu)

## Slide 12: Evaluation (2)
For accomplishment of MSTR fuel cycle requirements, implementation of another pyrochemical separation methods will be necessary.
Possible methods:
  Reductive extraction from molten fluoride salt into molten metal
    Group selective method for removal of both An’s and Ln’s from the melt in reduced form dissolved in liquid metallic phase
  Anodic dissolution of reduced metals and their electrotransport to solid or liquid cathode
    Group selective method usable for prior removal of Ln from mixture of reduced Ln’s + An’s

## Slide 13: Proposed scheme of MSTR Fuel Cycle: Back-end
Multi-stages
Electroseparation: Anodic dissolution
LiF - BeF2 - NaF +
LnFx + AnFx + FPx
Waste
M (l) + NM
Reducing agent (Li)
Molten Metal (M = Cd, Bi)
LiF - BeF2 - NaF + non-reduced matters
MSTR
Multi-stages
Salt / Metal Extraction
M (l) + An, Ln + FP
An
Fluoride melt
Fluoride melt
+ impurities
Ln, FP
Electroseparation: Cathodic deposition
impurities
Distillation
NM
Fuel Processing Unit
Fresh Fuel
HF